發表論文全文

年   月   日

| 報告人姓名 | 霍正邦 | 就讀系所及年級 | 機電系博士班二年級 |
| --- | --- | --- | --- |
| 發表論文全文： 若同學已有PDF檔之論文可將檔案名稱改成”發表論文全文.PDF” 即可直接上傳，不需使用此表格 Investigation of the Interfacial Reaction between Optical glasses and Various Protective Films and Mold Materials C.L. Chao1, C.B. Huo1, W.C. Chou1, T.S. Wu1, K.J. Ma2, Y.T. Chen3, C.W. Chao4 1Department of Mechanical and Electro-Mechanical Engineering, Tam-Kang University, No.151 Ying-Chuan Road, Tamsui, Taipei Hsien, Taiwan 251 2Department of Mechanical Engineering, Chung Hua University, No. 707, Sec. 2, Wu Fu Rd., Hsin Chu, Taiwan 30067 3Department of Mechatronic, Energy and Aerospace Engineering, National Defense University, No. 190, Sanyuan 1st St., Tahsi, Taiwan 33508 4Department of Information Management, Hsing-Wu College, Lin-Ko, Taiwan Glass molding process(GMP) is regarded as a very promising technique for mass producing high precision optical components such as spherical/ aspheric glass lenses and free-form optics. However, only a handful of materials can sustain the chemical reaction, mechanical stress and temperature involved in the glass molding process. Besides, almost all of these mold materials are classified as hard-to-machine materials. This makes the machining of these materials to sub-micrometer form accuracy and nanometer surface finish a rather tough and expensive task. As a result, making mold life longer has become extremely critical in the GMP industry. The interfacial chemical reaction between optical glass and mold is normally the main reason for pre-matured mold failure [1][2]. This research aimed to investigate the interfacial chemical reaction between various optical glasses, different anti-stick coating designs and several mold materials. The results showed that glass composition, coating design (composition, microstructure, thickness..), environment (vacuum, air or in protective gas), reaction temperature and time could all have profound effects on the interfacial chemical reaction. Based on the results, a design developed specially for certain glasses is more likely to be the viable way of optimizing the effect of the protective coating. [1] A. Jain, G.C. Firestone, and A.Y. Yi, J. Am. Ceram., 88 [9], p.2409 (2005). [2] K.J. Ma, H.H. Chien, C.L. Chao and K.C. Hwang, Key Engineering Materials, Vols. 364-366, p.655 (2008). |

註：請以12字大小繕打